Adsorption of Fluorinated Greenhouse Gases on Activated Carbons: Evaluation of their Potential for Gas Separation

This work was presented at the 3rd ANQUE-ICCE International Congress of Chemical Engineering (2019, Santander, Spain)

Julio E. Sosa,a,‡ Carine Malheiro,b,‡ Rui. P. P. L. Ribeiro,a Paulo J. Castro,a Manuel M. Piñeiro,c João M. M. Araújo,a Frédéric Plantier,b José P. B. Mota, a,* and Ana B. Pereiroa,*

aLAQV, REQUIMTE, Department of Chemistry, Faculdade de Ciências e Tecnologia, Universidade Nova de Lisboa, 2829-516 Caparica, Portugal

bUniversité de Pau et des Pays de l’Adour, E2S UPPA, CNRS, TOTAL, LFCR, Anglet, France

cDepartamento de Física Aplicada, Facultade de Ciencias, Universidade de Vigo, E36310 Vigo, Spain

‡These authors are equally contributing authors.

*Corresponding authors’ e-mail: anab@fct.unl.pt (A.B. Pereiro), pmota@fct.unl.pt (J.P.B. Mota), Fax: (+351) 212948550; Tel: (+351) 212948318.

ABSTRACT

BACKGROUND: The increasing awareness of the release of fluorinated gases (F-gases) into the atmosphere is instigating the development of techniques to capture them from refrigerants. In this work, the adsorption of difluoromethane (R-32), pentafluoroethane (R-125), and 1,1,1,2-tetrafluoroethane (R-134a) on four different activated carbons (ACs) is studied. Additionally, the selectivity of the ACs for the components of commercial refrigerants, R-410A and R-407F, is evaluated.

RESULTS: The estimation of the density of the adsorbed phase as a function of temperature allows the experimental fractional loading of each F-gas on any of the ACs to be correlated as a temperature-independent function of its reduced pressure, which is described by Toth or dual-site Langmuir equations or as an exponential function of the adsorption potential under the Adsorption Potential theory (APT). It is shown that the APT can be generalized with excellent accuracy to the systems studied if an adsorbate-dependent affinity coefficient is used as a shifting factor to bring the characteristic curves of F-gases into a single one for each AC. R-32 is the F-gas more adsorbed by all adsorbents, followed by R-134a, and by R-125. All ACs are selective for R-125 in R-410A commercial refrigerants, specially at lower pressures. Additionally, all ACs are selective for R-125 and R-134a over R-32 in R407-F commercial refrigerant.

CONCLUSION: The utilization of ACs for adsorption of the three most used F-gases is promising. By selecting ACs with different porous characteristics, it is possible to evaluate their influence on the selectivity for the components of different commercial refrigerants.

KEYWORDS. Adsorption, activated carbons, fluorinated gases, adsorption equilibrium.

INTRODUCTION

Fluorinated gases (F-gases), including hydrofluorocarbons (HFCs), perfluorocarbons (PFCs), and sulfur hexafluoride (SF6), are man-made greenhouse gases with a wide range of industrial applications (e.g. refrigeration, fire extinguishers, and solvents).1 These gases are energetically efficient, do not damage the ozone layer, and have low levels of toxicity and flammability.2 Following the Montreal Protocol, the ozone-depleting chlorofluorocarbons (CFCs) and hydrochlorofluorocarbons (HCFCs) were phased out and F-gases have mostly replaced them. F-gases emissions have increased 60% since 1990 and it is predicted that the HFC emissions will grow 140% between 2005 and 2020.3,4 However, these gases are major contributors to global warming, with a global warming potential (GWP) up to 23,000 times higher than that of CO2, and may persist up to 50,000 years in the atmosphere.1,2,5 Due to the EU commitments to the Kyoto’s Protocol, the use of F-gases has been regulated and controlled since 2006.The aim is to cut the overall greenhouse gas (GHG) emissions by 80-95% compared to 1990 levels by 2050.4 Additionally, the Kigali international agreement (2016) established the first international regulation to decrease F-gases emissions.6,7

The third-generation refrigerants include the commonly used R-134a (1,1,1,2-tetrafluoroethane) and mixtures containing R-32 (difluoromethane), R-125 (pentafluoroethane), and R-134a, such as R-407F and R-410A. These refrigerants have high GWP and will be phased out.6 They are being replaced by fourth-generation refrigerants which includes hydrofluoroolefins (HFO), as pure refrigerants, or in blends with HFCs in a reduced proportion. The fourth-generation refrigerants present significantly lower GWP. R-444A, R-447A, and R-448A are examples of blends of HFOs with R-32, R-125, R-134a, and other HFCs, that are being considered for refrigeration purposes.8

Taking this information into account, the separation and recovery of F-gases from third-generation refrigerants is of vital importance, not only to avoid their release into the atmosphere but also to recycle them and to produce blends with HFOs (fourth-generation refrigerants), applying circular economy, a priority in Europe. Currently, few technologies based on expensive processes such as cryo-condensation or membrane separation have been utilized to partially recover F-gases.9 However, technologies that efficiently separate and recover these F-gases have not yet been commercialized. Thus, it is vital to develop sustainable processes based on the utilization of environmentally benign materials to capture, recover, and recycle F-gases.

This work aims to study the capture by adsorption of the three most commonly employed pure F-gases in domestic refrigeration (R-32, R-125, and R-134a). The adsorption of these gases on activated carbons (ACs), zeolites, or metal-organic frameworks (MOFs) at various temperature and pressure ranges has been reported in literature.10-31 Even though MOFs present in general higher adsorption capacities, ACs are the most commonly used adsorbents in many industrial processes due to their large micropore and mesopore volumes, high surface area, variety of surface functional groups, low cost, and wide range of available morphologies.32,33

In this work, four ACs, two of which are commercially available, with different porous characteristics (e.g. total pore volume and pore size distributions - PSDs) were chosen to study F-gases adsorption. The two commercial ACs (Ecosorb and BAC) are widely used for solvent recovery, air treatment and purification, and many other applications. The two non-commercial ACs (AC1 and AC2) were designed to have high adsorption capacity, fast adsorption kinetics, good thermal conductivity, and minimal sieving effects for large impurities. Besides, both AC1 and AC2 have been previously characterized and the latter has also been studied before for gas adsorption and separation.32-34

The adsorption of R-32,10,26 R-125,24,25 R-134a,14-17,19,20,27-29 and of commercial refrigerants containing these F-gases30,31 on other ACs has been already studied in the literature. However, to the best of our knowledge, this work is the first publication reporting on a systematic study of the adsorption of those three pure F-gases on four different ACs with different porous characteristics in order to select the best material for the separation of commercial refrigerants.

The adsorption equilibrium of R-32, R-134a and R-125 on the four ACs at 283.15 K, 303.15 K and 323.15 K were measured and compared. The experimental single-component adsorption equilibrium data were successful correlated using dimensionless forms of the Tóth and dual-site Langmuir models. Furthermore, the Adsorption Potential theory not only correlated well the experimental adsorption data, but also allowed to superimpose the adsorption data of all the F-gases on each AC into a single, temperature-independent characteristic curve.

Since different F-gases refrigerants are used industrially, the selective separation of different F-gases from gas mixtures is also crucial. Thus, the Ideal Adsorption Solution theory (IAST) was used to predict the adsorption equilibria of two multicomponent commercial refrigerants, R-410A (a mixture of equal weights of R-32 and R-125) and R-407F (a mixture of R-32, R-125, and R-134a), on the studied ACs. Moreover, the selectivity of these adsorbents for the components of the gas mixtures at different equilibrium gas phase compositions and pressures was evaluated. This work presents a step forward in the study of F-gases adsorption onto porous solid matrices and in the still poorly explored area of the capture and separation of F-gases from commercial refrigerants.

MATERIALS AND METHODS

Materials

Difluoromethane, R-32 (wt-% purity ≥ 99.9), and 1,1,1,2-tetrafluoroethane, R-134a (wt-% purity ≥ 99.8), were supplied by Linde, and pentafluoroethane, R-125 (wt-% purity ≥ 99.8, was supplied by Sepim. The designation and chemical structure of these F-gases are shown in Table 1. Helium (wt-% purity ≥ 99.999) was supplied by Praxair.

The two noncommercial ACs, referred here to as AC1 and AC2 were developed and produced by Sutcliffe Speakman Carbons Ltd. (UK). AC1 is a granular coconut shell carbon and AC2 is an extruded carbon coal based (2 mm diameter pellets). Ecosorb activated carbon, in form of pellets (4 mm diameter), was supplied by Jacobi, and BAC bead-shaped activated carbon (0.70 mm average diameter) was supplied by Kureha.

Experimental Procedure

The nitrogen (N2) adsorption isotherm at 77 K in each AC was determined in a Micromeritics ASAP 2020 apparatus (Fig. S1 of Supporting information). The specific surface area (SBET) was estimated with the BET method. The pore size distribution (PSD) and the pore volume of each sample were determined by deconvolution of the N2 adsorption isotherm at 77 K using standard methods based on the Non-Localized Density Functional theory.35

The single-component adsorption equilibrium isotherms for R-32, R-125, and R-134a on the four ACs were measured using a standard gravimetric method at 283.15 K, 303.15 K, and 323.15 K, and at pressures up to 1.5 MPa (the maximum ratio applied for pressure/saturation pressure was of 0.78 for R-32, 0.88 for R-125, and 0.79 for R-134a). This method consists of the stepwise supply of pure F-gas to a temperature-controlled measurement cell containing the adsorbent (ca. 0.5–0.7 g), while the mass and pressure variations are monitored until equilibrium is reached. Adsorption/desorption cycles were performed to check for the presence of hysteresis.

Adsorption measurements were performed, as described elesewhere,36-38 in a high-accuracy IsoSORP high-pressure magnetic-suspension balance (MSB) (Rubotherm GmbH, Germany, maximum load of 25 g, resolution of 10 µg, uncertainty less than 0.002%, and reproducibility  smaller than  3×10−5 g). The experimental setup is schematized in Fig. S2 of Supporting information. This type of balance uses a measurement method based on the mechanical equilibrium between a magnetic force, sample weight, and buoyancy effect.39,40 The temperature was kept constant by using a thermostatic bath (uncertainty of ± 0.1 K). The pressure was measured with transducers working with accuracy over the full range of operation pressures: a Baratron model 627D (MKS Instruments GmbH, Germany) for 0–0.1  MPa, accuracy of 0.12 %; two Omegadyne Inc. (Sunbury, OH, USA) models PX01C1-150A5T and PX01C1-500A5T, respectively for 0–1  MPa and 0–3.5 MPa (both with accuracy of 0.05 % of the full scale). The equilibrium was considered to have been attained when pressure and mass changes in the system were no longer observed. Before the measurements, the AC samples were degassed for at least 12 hours under vacuum at a minimum of 373.15 K.

The adsorption equilibria data are reported in terms of excess adsorption, qex, defined as

qex=w-ms+Vhρgms+vsρg                                                                                                               (1)

where w is the apparent mass weighed by the balance, ms the degassed mass of AC sample in the measurement cell, Vh the cumulative volume of all physical parts in the measuring cell contributing to buoyancy effects, ρg the density of the gas at the equilibrium pressure and temperature of the experiment, and vs the specific volume of the adsorbent impenetrable to the adsorbate (vs=1/ρs, where ρs is the density of the solid matrix of the adsorbent). The solid density ρs was determined experimentally by helium (He) picnometry (assuming He behaves as a non-adsorbing probe molecule).

Excess adsorption can be converted to total adsorption, q, via

q=qex1-vaρg                                                                                                                                           (2)

where va (cm3/mol) is the specific (or molar) volume of the adsorbed phase. It is usually assumed that for (subcritical) adsorption from the vapor phase va can be approximated by the specific (or molar) volume, vm, of the saturated liquid adsorptive at the adsorption temperature.41 In this work, however, va has been determined more accurately from the temperature-dependent saturation capacity of the adsorbent estimated in the framework of the Adsorption Potential theory. This procedure is detailed below.

The gas density, ρg(T,P), can be determined experimentally with the MSB by measuring the buoyancy effect exerted by the gas on a calibrated volume with known mass and density, but it can also be calculated with an appropriate equation of state, or even extracted from the NIST Chemistry Webbook.42 In the present work the latter method was adopted. The uncertainty39 of the calculated adsorbed mass is around 1% over the full range of temperature and pressure.

The differential heat of adsorption, Qst, of each AC was determined using a homemade apparatus coupling manometric and calorimetric techniques, whose scheme is shown in Fig. S3 of Supporting information. This apparatus, detailed by Mouahid et al.,43 allows the simultaneous measurement of Qst and the equilibrium amount of gas adsorbed at a given temperature and pressure. Briefly, gas is injected into a dosing cell, which is connected to an adsorption cell containing the adsorbent. As the gas is adsorbed it releases heat, which is recorded. A material balance before and after the connection of the dosing and adsorption cells gives the amount of adsorbed gas. At the same time, the recorded heat peak gives information about the total heat flow (Q), which is the sum of the integral heat of adsorption, Qa, and of the heat of compression (Qc) due to the gas injection into the adsorption cell. Qa is then calculated from

Qa=Q-Qc                                                                                                                                            3

where Q is directly estimated by integration of the heat peak and Qc given by43

Qc=-VeTαp-αssΔP                                                                                                                      4

where Ve is the volume considered by the thermopiles and is calculated from helium calibration, αp the isobaric expansion coefficient, αss the isobaric coefficient of the stainless steel of the calorimeter, and ΔP the difference between the equilibrium pressure of the measured point and the previous one. The differential heat of adsorption is then approximated by

Qst=Qa∆q                                                                                                                                                  5

where ∆q is the amount of gas adsorbed between the two consecutive pressure steps. The overall uncertainty43 in the measurement of Qst is less than 5%.

RESULTS AND DISCUSSION

Materials Characterization

F-gas adsorption was studied on four ACs with different textural characteristics, of which two are commercially available. The specific BET surface area, SBET, and specific pore volume, vp, of each AC are listed in Table 2 and the PSDs depicted in Fig. 1. The SBET value determined AC1 (1695 m2/g) is in reasonable agreement with the previously reported data (1669 m2/g),34 while the value of AC2 (1280 m2/g) is slightly lower than previously reported (1342 m2/g).32,34

Despite the similar values of SBET and vp for the two commercial ACs (Ecosorb and BAC), their different PSDs (see Fig. 1) influence the capture of F-gases. While Ecosorb has a polydisperse PSD in the micropore (pores smaller than 20 Å) and mesopore (pore diameters between 20 Å and 500 Å) regions, BAC has a narrower pore size distribution lying in the micropore region with a peak around 10 Å (see Fig. 1). The two non-commercial ACs have larger values of SBET and vp (see Table 2) than BAC and Ecosorb, which favor gas adsorption. While AC1 has a polydisperse PSD in the micropore and ultra-micropore (pore size smaller than 10 Å) regions, the PSD of AC2 also extends into the mesopore regions (see Fig. 1).

Adsorption Equilibrium of F-gases on ACs

The experimental adsorption equilibrium data at 283.15 K, 303.15 K, and 323.15 K, expressed as milimoles of adsorbed gas per gram of adsorbent (mmol/g), are plotted in Figs. 2–4 as a function of the applied equilibrium gas pressure (see also Tables S1–S12 of Supporting Information). The maximum adsorption pressures for each studied F-gas was around 15% lower than its vapor pressure at 283.15K (0.77 MPa for R-134a, 1.57 MPa for R-125, and 1.93 MPa for R-32). The isosteric heat of adsorption for each AC/F-gas pair was measured at 323.15 K (Fig. 5).

The adsorption data were analyzed in the framework of the Adsorption Potential theory (APT), for it is assumed that the main mechanism governing subcritical F-gas adsorption in essentially microporous ACs is pore filling.44-46According to this theory the specific volume of adsorbed phase, W (cm3 of adsorbed phase per gram of AC), is a function solely of the adsorption potential, ϕ:

W≡qva=Wϕ                                                                                                                                  6

where Wϕ is a temperature-independent characteristic curve for each solid–fluid system. The adsorption potential is defined as

ϕ=μs-μ=RT lnfsf      f≤fs                                                                                                   7

where R is the ideal gas constant, T the system temperature, f the fugacity of the gas at the equilibrium pressure and temperature, fs its saturation fugacity at the same temperature, and μ and μs are the corresponding chemical potentials. All fugacity values were determined using the Aspen Plus v.10 database.

The characteristic curve, Wϕ, should be a positive monotonic decreasing function of ϕ satisfying the two limits

limϕ→0θ=1,    limϕ→∞θ=0                                                                                                                       8

where θ≡W/Ws is the fractional loading or pore volume filling and Ws is the specific pore volume of the adsorbent accessible to the adsorbate, taken to be equal to the corresponding value of vp listed in Table 2.

Although va is usually approximated by vm, it is known that the force field exerted by a micropore compresses the adsorbed phase beyond that of a saturated liquid. Although this effect is small at temperatures well below the critical value, Tc, of the adsorbate, it should be more pronounced as the temperature approaches Tc, i.e.,

αT=vavm                                                                                                                                               9

should be a monotonic decreasing function of T as the latter is increased up to the critical value.

In this work a more accurate estimate of va is obtained by calculating it in such a way that the expression

vaT=limP→Ps(T)vp/q(T)≡vp/qs(T)                                                                                   (10)

where qsT is the saturation capacity of the adsorbent, results in a temperature-independent Wϕ curve. This procedure, an example of which is shown in Fig. 6 for R-32 adsorption on AC2 (similar graphs for the other AC/F-gas combinations are included in Figs. S4 and S5 of Supporting Information), serves two purposes: (i) it produces a single, temperature-independent characteristic curve with minimum data scatter and (ii) corrects the limiting behavior of Wϕ so that it satisfies the condition limϕ→0θ=1 when Ws is equal to the specific pore volume, vp. In Figs. S4 and S5 of Supporting Information, which include similar graphs for the other AC/F-gas combinations, there are several cases where the effectiveness of the proposed procedure is striking.

It was found that for all studied solid-fluid systems αT is very well approximated by a linear function

α=α1-α2T                                                                                                                                   (11)

where α1 and α2 are constants specific of each AC/F-gas pair, or, alternatively, va(T) can be fitted directly to an expression of the type

lnva=a-bT                                                                                                                                       12

where a and b are fitting parameters. The values of α, va, and vm (the latter obtained as a function of T from the NIST Chemistry Webbook42) are listed in Table S13 of the Supporting Information. The average value of α over all studied solid-fluid systems and temperatures is 0.89 with standard deviation of 0.08, which indicates that the adsorbed phases are slightly more compressed than the saturated, liquefied F-gases.

Interestingly, it turns out that a graph of θ as a function of the reduced pressure x=P/Ps, obtained using the estimated values of va, merges quite nicely in a single master curve the three experimental adsorption isotherms for each of the twelve AC/F-gas systems studied. Fig. 7 shows a representative example of such plot for R-32 adsorption on AC1 (similar graphs for the other AC/F-gas combinations are included in Figs. S6 and S7 of Supporting Information).

Single-component adsorption equilibrium data are commonly fitted to classical thermodynamic models for predicting multicomponent, competitive adsorption equilibria and for applying in model-based process design.47 One of the most often used models is that of Tóth,48 which is described by

q=q∞bP1+bPt1/t                                                                                                                             13

where q∞=logP→∞q, b=H/q∞ an affinity constant (bar-1), H (mmol g-1 bar-1) the Henry constant, and t a dimensionless heterogeneity parameter. The temperature dependencies of the parameters b and t are usually defined as

b=b0expQRT                                                                                                                                 14

t=t0+B1-T0T                                                                                                                           15

where b0 is the value of the affinity constant at infinite temperature, Q a measure of the isosteric heat of adsorption, t0 the value of the heterogeneity parameter at a reference temperature T0, and B the slope of the plot of t versus -1/T.

It is worth noting that the Tóth model is much more suitable for modeling supercritical rather than subcritical adsorption equilibria. Although the Tóth model returns a value of q for any arbitrarily large value of P, for subcritical adsorption—as is the case here—it makes no sense to go above the saturation pressure, Ps, of the adsorptive at the adsorption temperature. In fact, in this case the parameter q∞ should be regarded as a fictitious saturation capacity that allows the model to satisfy the condition q(T,Ps)=qs≡vp/va. For this condition to be met q∞ must be defined as

q∞=qs1+bPst1tbPs                                                                                                                         16

and in this case the Tóth model can be expressed in the following dimensionless form that relates the fractional loading and the reduced pressure:

θ=1+b't1+b'xt1/tx                                                                                                                         17

where b'=bPs. Given that the representations of θ as a function of x for the studied AC/F-gas combinations result in (nearly) temperature-independent curves, eqn. 17 can be fitted directly to those data with just two temperature-independent parameters (b' and t)—this is quite convenient.

Away from the critical temperature and not too high vapor pressures of the adsorptive, the temperature-dependence of Ps is given by the simplified form of the Clausius-Clapeyron equation

Ps=Ps∞exp-∆HvRT                                                                                                                         18

where ∆Hv is the specific enthalpy of vaporization. Combining this expression with eqn. 14, it is concluded that the parameter Q in eqn. 14 must be equal to ∆Hv for b'≡bPs to be independent of temperature.

Another useful single-component adsorption equilibrium model is the multi-site Langmuir model,41 which can be written as

q=k=1nsHkP1+bkP                                                                                                                            19

where Hk is the contribution of sites (or pores) of type k to the overall Henry constant, H=Hk, and bk the corresponding Langmuir equilibrium constant. Since the model must satisfy the constraint qPs,T=qs(T), it is convenient to rearrange it in dimensionless form as follows

θ=k=1nsθk(1+bk)x1+bkx,  θ1+⋯θns=1                                                                             20

where the Henry constants have been replaced by the fractional site distributions, θk. In particular, for ns=2 the above expression reduces to the dual-site (or bi-)Langmuir model

θ=θ1(1+b1)x1+b1x+1-θ11+b2x1+b2x                                                                                        21

This three-parameter model is the simplest of the series capable of describing the heterogeneity of an activated carbon, in which, for example, θ1 and b1 characterize the contribution of the smaller pores and 1-θ1 and b2≪b1 that of the larger ones.

Under the ATP framework the experimental characteristic curve, W(ϕ), is commonly fitted to the Dubinin–Astakhov (D–A) equation.46,49,50

W=Wsexp-γϕn                                                                                                                                        (22)

where γ and n are fitting parameters related to the characteristic energy for the given adsorbent and to the pore size distribution, respectively. However, we have found that the alternative approach of fitting W(ϕ) to a low-order polynomial expansion,49

ln⁡(W/Ws)=γ1ϕ+γ2ϕ2+γ3ϕ3+⋯                                                                                                          (23)

where the γ’s are fitting parameters, usually describes better the experimental data.

To obtain the isosteric heat of adsorption, Qst, for a given adsorption isotherm model, one uses the relationship Qst=RT2∂lnP/∂Tq, analogous to the well-known Clausius–Clapeyron equation for a one-component gas-liquid system. The result for the dimensionless Toth model defined by eqn. 17 is

Qst=∆Hv-Rγ1+bn1+bn-bθn                                                                                                     24

where ∆Hv and γ≡dlnva/d(1/T) are constants if the explored temperature range is not too wide. Since γ<0, eqn. 24 defines Qst as a monotonically increasing function of θ limited between Qst0=∆Hv+Rγ and Qst1=∆Hv+Rγ(1+bn).

The isosteric heat of adsorption for the dimensionless dual-site Langmuir model, given by eqn. 21, is very well (though not exactly) approximated by

Qst=∆Hv-Rγ1+θ1b1+1-θ1b21+θ1b1+1-θ1b21-θ                                                                      25

which is as a monotonically increasing function of θ from Qst0=∆Hv+Rγ to Qst1=∆Hv+Rγ1+θ1b1+1-θ1b2.

Finally, for the APT model given by eqn. 6 the isosteric heat of adsorption is

Qst=∆Hv+ϕξ+γξθTdϕdθ                                                                                                                   26

where ξ≡dln(fs/f)/dln(Ps/P), which is slightly smaller than 1, can be taken as constant with very good approximation if the explored temperature range is not too wide. Although T appears explicitly in eqn. 26, it is worth noting that the latter expresses Qst as a function of θ because ϕ/T=-Rlnx, where x is the reduced pressure, and it was observed that θ=θ(x) for the solid-fluid systems studied. According to eqn. 26, at low fractional loadings Qst is approximately given by Qst=∆Hv+ϕ/ξ, which is a monotonically decreasing function of θ starting from the limiting value Qst0≡limθ→0Qst=+∞, whereas at high fractional loadings Qst=∆Hv+(γ/ξT)(dϕ/dlnθ), which is an increasing function of θ. The overall result is that Qst(θ) will have a more or less convex shape.

The dimensionless Tóth parameters that best fit the experimental adsorption data for each AC/F-gas pair are listed in Table S14 of Supporting Information and the corresponding fittings are plotted in Figs. 2–4 as dashed lines. The experimental adsorption data for each AC/F-gas pair were also successfully fitted to the dimensionless dual-site Langmuir model (the parameters are listed in Table S15 and the corresponding fittings plotted in Figs. S8 to S10 of Supporting information), as well as to the APT model in the form of eqn. 23 (Table S16 and Figs. S11-13 of Supporting Information). These models have been chosen because they correlate well adsorption equilibrium data at low and high pressures on heterogeneous adsorbents such as activated carbons. The good agreement between the fittings of the three different adsorption equilibrium models and the experimental adsorption data shows that these models describe well the thermodynamics of the studied AC/F-gas systems and are therefore suitable for use in modeling and simulation of adsorption-based separation processes. Additionally, it was observed that replacing the fractional site-distribution parameter, θi,1, for adsorption of F-gas i in a given AC, by a single adsorbate-independent parameter, θ1, did not change the quality of the fitting but increased its robustness. Table S17 of Supporting Information lists the best-fit parameter values of this model for each of the twelve solid-fluid systems.

Overall, both Tóth’s and the dual-site Langmuir model fit equally well the experimental adsorption data; they are, however, slightly outperformed by the APT model when it is formulated in the form of eqn. 23.

Each adsorption isotherm (Figs. 2–4) exhibits the classical Type I behavior51 of gaseous adsorbates in microporous solids, with progressive pore filling due to the polydisperse PSD. At the highest pressures tested at 303.15K the adsorption capacity for R-32 is 9.48 mmol/g on Ecosorb, 9.32 mmol/g on BAC, 14.5 mmol/g on AC1, and 12.4 mmol/g on AC2. For R-134a in the same conditions, the adsorption capacity is 5.95 mmol/g on Ecosorb, 5.83 mmol/g on BAC, 9.26 mmol/g on AC1, and 8.36 mmol/g on AC2. For R-125 in the same conditions, the adsorption capacity is 5.23 mmol/g on Ecosorb, 5.67 mmol/g on BAC, 9.15 on AC1, and 7.72 mmol/g on AC2. The two noncommercial ACs (AC1 and AC2) have larger adsorption capacities at higher pressures, which is in accordance with their higher surface area and pore volume.

All ACs have similar Qst values for each gas (see Fig. 5), with slightly larger values for R-125 and R-134a than for R-32, and all of them strongly correlated with the respective heats of vaporization. The isosteric heats of adsorptions calculated from the dimensionless Tóth, dimensionless dual-site Langmuir, and APT models are plotted and compared with the experimental calorimetric data in Figs. S14 and S15 of Supporting Information. The predicted Qst values are in fairly good qualitative—if not quantitative—agreement with the measurements, but far from the fine quality by which the equilibrium loadings are described by the same thermodynamic models. In accordance with the observations on the fittings of the adsorption measurements, the APT model seems to describe the measured Qst data better than the other two models. This is not surprising, given that the APT model is the only one of the three capable of describing the monotonically decreasing or concave shapes of the experimental Qst curves.

In order to evaluate the adsorption capacities of each AC, the adsorption isotherms of R-32, R-125, and R-134a at 303.15 K on the four ACs were compared (Supporting information, Fig. S16). At the highest pressures, R-32 is the most adsorbed F-gas on all ACs, followed by R-134a, and then by R-125. This results from the adsorption of a vapor close to conditions of complete pore filling being governed by the entropy of its liquid-like adsorbed phase and, therefore, the saturation capacity, qs=vp/va, being approximately inversely proportional to the molar volume, vm, of the condensed adsorptive at the adsorption temperature, due to the dependence of qs on va. This is indeed the case given than the ordering of the vm’s is R-32<R-134a<R-125.

Since the four ACs have different PSDs, the experimental adsorption data were interpreted taking the specific surface area and pore volume of each AC (listed in Table 2) into account. Fig. S17 of Supporting information compares the experimental adsorption equilibria of R-134a at 323.15 K on the different ACs, expressed as the amount adsorbed per unit weight of solid (mmol/g), unit surface area of solid (mmol/m2), and unit pore volume of solid (mmol/cm3). On a weight basis, the noncommercial AC1 carbon has much higher adsorption capacity at higher pressures than the commercial BAC and Ecosorb carbons, followed by AC2. However, when the results are compared per unit surface area or unit pore volume of solid, the performance difference between the carbons clearly decreases, as expected. The best results, obtained at high pressures, for AC1 and AC2 are due to their larger porous volumes, which lead to a higher adsorption capacity. Similar observations can be made for the other AC/F-gas pairs at 298.15 K, 303.15 K, and 323.15 K (data not shown).

On the other hand, in the low-pressure region the free energy of the AC/F-gas system is totally governed by enthalpic effects, as the Henry constant is solely a function of the solid-fluid interaction potential. The latter is a strong function of pore width, decreasing with increasing pore size in the micropore range and then levelling off at the value for the interaction with a single flat carbon wall. Additionally, the contribution of a given pore width to the total amount adsorbed in the low-pressure region will be proportional to the contribution of that pore size to the specific surface area of the solid. Hence, the importance of the PSD for analysis of the low-pressure F-gas adsorption data on the ACs. Indeed, such an analysis shows that the AC with larger pores in the micropore range (AC2) has lower adsorption capacity in the low-pressure region than the other ACs with smaller pore sizes.

Generalization of the Results

The APT has two attributes especially useful for predicting single-component adsorption equilibrium from a limited set of experimental measurements. The first one, which has been amply demonstrated above, is that according to the theory the characteristic curve is temperature independent. Therefore, only adsorption equilibrium measurements at one temperature are necessary to obtain the characteristic curve, and this is sufficient to describe the adsorption at all temperatures for the same gas-solid system. The second feature, despite being of more limited applicability, is also very useful: in many cases the theory can be generalized if an adsorbate-dependent affinity coefficient, β, is used as a shifting factor to bring the characteristic curves of all gases on the same adsorbent into a single curve. This has been observed to hold for a series of systems32,37,52 and it is demonstrated here that it can also be generalized with excellent accuracy to the twelve solid-fluid systems studied.

Introducing an adsorbate-dependent affinity coefficient, βi, as a scaling factor of the adsorption potential for the ith F-gas leads to

Wi≡qvai=Wϕi,  /,ϕi≡ϕiβi                                                                                          27

where W(ϕ) is a function supposed to be adsorbate independent. Following previous work,53-54 the affinity coefficient is assumed to be a power function of the molecular parachor, P (a measure of molecular volume), that is

βiβj=PiPjn                                                                                                                                          28

where n=0.9 is the most suggested exponent. Following the usual convention of setting β=1 for benzene (P=199.0), the previous equation takes the form βi=(Pi/199.0)0.9. In the present work P is approximated by the simple formula P=8.0+0.707Vc,34 where Vc is the critical volume (taken from the NIST Chemistry Webbook42).

The APT was successfully applied to the adsorption equilibrium data of R-32, R-125, and R-134a on the four ACs, to obtain a single temperature-independent characteristic curve for each solid-fluid system. Moreover, by employing the β coefficient it was possible to collapse the characteristic curves of the different F-gases on the same AC into a single characteristic curve (Fig. 8). It should be highlighted that these characteristic curves were generated without any fitting of the β parameters—they are among the multi-adsorbate characteristic curves with the lowest data dispersion reported in the literature since Dubinin's pioneering work in the mid-1940s.55 These characteristic curves were fitted to eqn. 23 with very good precision (Fig.8); the fitted parameters are listed in Table S16 of Supporting Information.

Prediction of mixed-Gas Adsorption using the Ideal Adsorption Solution Theory

Near azeotropic mixtures of F-gases, such as the commercial refrigerants R-410A and R-407F, are not easily separated into their individual components by distillation. The selectivity of an adsorbent towards one component from a gas mixture is critical to develop highly efficient adsorbent-based gas separation processes.

From the fittings of the Tóth model to the single-component adsorption equilibrium data of the three F-gases, the Ideal Adsorption Solution theory (IAST)56 was used to predict the multicomponent adsorption equilibrium of R-410A (R-32/R-125, 50/50 wt%) and R-410F (R-32/R-125/R-134a, 30/30/40 wt%), and also the mole-fraction composition of their adsorbed phases. It should be noted that a similar procedure based on the fittings of the dual-site Langmuir or APT models could very well have been adopted — the choice of Tóth’s model was a simple matter of convenience.

Although the IAST is well explained elsewhere,56,57 it is worth noting that for multicomponent adsorption of a condensable vapor the hypothetical single-component fugacity, fi0(π'), of the ith component of the mixture that gives the same spreading pressure, π', on the surface of the adsorbent as those of all other components should be computed as

π'RT=0fi0qi0Pi,T dlnfiif  fi0<fis 0fisqi0Pi,T dlnf+qislnfis/fi0if  fi0>fis                                                      29

where qi0Pi,T and qis are the single-component adsorption isotherm and saturation capacity at temperature T, respectively, and Pis the vapor pressure of the pure component at the same temperature. This correction is due to the fact that if the hypothetical single-component pressure Pi0 exceeds Pis (or the corresponding hypothetical pure-component fugacity fi0 exceeds fis), the adsorbed quantity should remain equal to qis.

The adsorption equilibria of R-410A and R-407F in the four ACs at 303.15 K were simulated for a pressure range between 0.01 and 0.8 MPa. The equilibrium mole fractions of the gas phase (y) correspond to the bulk compositions of the two commercial F-gases (yR-32(0)=0.7 and yR-125(0)=0.3 for R-410A, and yR-32(0)=0.47, yR-125(0)=0.21, and yR-134a(0)=0.32 for R-407F). The results are plotted in Fig. S18 and shown in Tables S18 and S19 of Supporting Information. Obviously, the isothermal adsorption of both gas mixtures increases with increasing pressure. The highest R-410A adsorption capacities were obtained for AC1 while the lowest adsorption capacities at the highest pressures were obtained for BAC and Ecosorb.

Simulations at four different total pressures (0.05, 0.1, 0.3, and 0.5 MPa) and varying the gas-phase equilibrium molar fractions were also performed for R-410A. The IAST predictions of the amounts of R-410A and its two components (R-32, R-125) adsorbed on the four ACs were performed as a function of yR-32 (Figs. S19–S22 and Tables S20–S23 of Supporting Information). As expected, the R-125 amount adsorbed decreases while the R-32 amount adsorbed increases when yR-32 is increased. Moreover, the equilibrium mole fraction of R-32 at which equal amounts of the two gases are adsorbed is always higher than 0.5 for all ACs, decreasing when the total pressure increases. This behavior indicates that the four ACs are more selective for R-125 than for R-32 and that this selectivity decreases with increasing pressure.

Selectivity of the ACs for F-gases in Binary and Ternary Mixtures

If the amount of free, unadsorbed gas in the pore volume of the adsorbent is negligible compared to the amount adsorbed, which is the case for the solid-fluid systems under consideration, the selectivity, Sij, of the solid for gas i over gas j is defined as

Sij=xi/xjyi/yj                                                                                                                                    (30)

where xi and xj are the mole fractions of i and j in the adsorbed phase, respectively, and yi and yj the mole fractions of i and j in the gas phase at equilibrium, respectively.

Using the IAST results, the selectivity, S12, of each carbon for R-125 (i=1) over R-32 (i=2) of the commercial refrigerant R-410A was determined. Therefore, if S12>1, R-125 is preferentially adsorbed, but if S12<1, R-32 is preferentially adsorbed. In Fig. S23 of Supporting Information S12 is plotted as a function of yR-32 for each activated carbon at 303.15 K. All ACs are more selective to R-125 than to R-32 at all tested pressures, and S12 increases at lower pressures. Moreover, at a given fixed pressure, S12 increases with increasing yR-32 for all carbons. The value of S12 was also determined as a function of pressure for the equilibrium gas-phase composition corresponding to that of bulk R-410A (Fig. 9). The results reinforce the observation that all ACs are selective to R-125, with the noncommercial ACs, AC1 and AC2, presenting the best selectivities. Although all ACs were selective to R-125 at all tested pressures, the highest S12 values were obtained at the lowest pressures.

In the case of the R-407F ternary mixture, the selectivities to R-134a (i=3) over R-125 (j=1) and R-32 (j=2), S31 and S32, and to R-125 over R-32, S12, were determined as a function of pressure at 303.15 K for the equilibrium gas-phase composition of the bulk R-407F (Fig. 10). All ACs are more selective to R-125 or R-134a than to R-32 and more selective to R-134a than to R-125. The highest selectivities were obtained for BAC (S12 and S32) and Ecosorb (S31). In general, all ACs are more selective to R-134a and R-125 than to R-32 and their selectivity is favored at lower pressures.

CONCLUSIONS

In the present work, the adsorption equilibrium of three of the most used F-gases in refrigeration was studied in four different types of activated carbon. The isosteric heats of adsorption were determined for each AC/F-gas. The adsorption data were successfully correlated with the Tóth, dual-site Langmuir, and APT models. The adsorption data of the three F-gases in each AC were successfully collapsed into a single temperature-independent characteristic curve. The experimental results show that the noncommercial activated carbons AC1 and AC2 have the highest adsorption capacities for the three pure F-gases studied at the highest pressures tested. Moreover, R-32 is the most adsorbed F-gas in all ACs.

Using the Ideal Adsorption Solution theory (IAST), the adsorption of two commercial gaseous refrigerant mixtures R-410A and R-407F was predicted at four different pressures and at different equilibrium gas compositions. The selectivity to each component of the mixtures was determined for the four activated carbons. All ACs are selective to R-125 in the R-410A commercial refrigerant, specially at low pressures, with one of the noncommercial ACs yielding the best selectivity. Additionally, all ACs are more selective to R-125 and R-134a than R-32 in the R407-F commercial refrigerant, with the commercial ACs presenting the best selectivities, specially at low pressures.

This work provides important insights into the fundamental understanding of the performance of different activated carbons for the capture and separation of F-gases from binary mixtures, such as the commercial refrigerant R-410A, and ternary mixtures, such as refrigerant R-407F. The use of activated carbons with different porous characteristics allows the selective adsorption of different F-gases from different F-gas mixtures. This information is of vital importance to understand which properties control the adsorption capacity of these materials. With this knowledge, the best material can be selected for application in the design and scale-up of a given separation process.

AUTHOR INFORMATION

Corresponding Author

*E-mail: anab@fct.unl.pt (A.B. Pereiro), pmota@fct.unl.pt (J.P.B. Mota), Fax: (+351) 212948550; Tel: (+351) 212948318.

ACKNOWLEDGMENT

The authors would like to acknowledge the funding of the KET4F-Gas project, SOE2/P1/P0823, co-funded by the Interreg Sudoe Programme through the European Regional Development Fund (ERDF). A.B. Pereiro and J.M.M. Araújo acknowledge FCT/MCTES for financial support through IF/00190/2014 contract and IF/00210/2014 contract, respectively. Rui Ribeiro acknowledges financial support through the Norma Transitória DL 57/2016 Program Contract (FCT/MCTES). This work was also supported by the Associate Laboratory for Green Chemistry – LAQV, which is financed by national funds from FCT/MCTES (UID/QUI/50006/2019).

SUPPORTING INFORMATION

Tables containing the adsorption equilibrium data (excess and total) of R-32, R-125, and R-134a in the activated carbons at 283.15 K, 303.15 K and 323.15 K; Table containing molar volumes of the saturated liquid and adsorbed phase and molar volume ratio for the solid-fluid systems; Tables and figures containing IAST simulations for adsorption of R-410A and of R-407F; Figures with the determination of αT for F-gas adsorption on activated carbons; Figures representing the fractional loading or pore volume filling, θ=WWs=qva/vp, as a function of reduced pressure, x=P/Ps, for F-gas adsorption on activated carbon; Figures with the isosteric heat of adsorption calculated from the dimensionless Toth, dual-site Langmuir and APT models together the corresponding experimental data; Figures representing the adsorption isotherms of the three refrigerants for each activated carbon; Comparison of experimental data of R-134a adsorption in the four activated carbons corrected for the pore volume and for superficial areas of the adsorbents; Figures representing the comparison between the isotherm data and the predictions obtained by applying the dual-site Langmuir and Dubinin–Astakhov (D–A) isotherm model; Figure representing selectivities of the activated carbons to the studied F-gas as a function of pressure of the commercial refrigerants R-410A and R-407F; Figures representing R-125/R-32 selectivity of the activated carbons to the studied F-gas as a function of the gas composition of the commercial refrigerant R-410A.

REFERENCES

- European Commission: Fluorinated greenhouse gases. https://ec.europa.eu/clima/policies/f-gas_en  (accessed July 31, 2019).

- United States Environmental Protection Agency: Overview of Greenhouse Gases. https://www.epa.gov/ghgemissions/overview-greenhouse-gases (accessed July 31, 2019).

- European Environment Agency. National emissions reported to the UNFCCC and to the EU Greenhouse Gas Monitoring Mechanism. Data Greenh Gas Emiss Removals, Sent by Ctries to UNFCCC EU Greenh Gas Monit Mech (EU Memb States) 2018.

- European Union. Regulation (EU) No 517/2014 of the European Parliament and of the Council of 16 April 2014 on fluorinated greenhouse gases and repealing Regulation (EC) No 842/2006 2014.

- European Environment Agency: EEA greenhouse gas - data viewer. https://www.eea.europa.eu/data-and-maps/data/data-viewers/greenhouse-gases-viewer (accessed July 31, 2019).

- Mota-Babiloni A, Makhnatch P, Khodabandeh R, Recent investigations in HFCs substitution with lower GWP synthetic alternatives: Focus on energetic performance and environmental impact. Int. J. Refrig. 82: 288-301 (2017).

- Heath E, Amendment to the Montreal Protocol on substances that deplete the ozone layer (Kigali Amendment). International Legal Materials, 56(1): 193-205 (2017).

- Mota-Babiloni A, Navarro-Esbrí J, Barragán-Cervera A, Molés F, Peris B, Analysis based on EU Regulation No 517/2014 of new HFC/HFO mixtures as alternatives of high GWP refrigerants in refrigeration and HVAC systems. Int. J. Refrig. 52:21-31 (2015).

- Shiojiri, K, Yanagisawa Y, Yamasaki A, Kiyono F, Separation of F-gases (HFC-134a and SF6) from gaseous mixtures with nitrogen by surface diffusion through a porous Vycor glass membrane. J. Membr. Sci. 282: 442–449 (2006).

- Askalany AA, Saha BB, Uddin K, Miyzaki T, Koyama S, Srinivasan K, Ismail IM, Adsorption Isotherms and Heat of Adsorption of Difluoromethane on Activated Carbons. J. Chem. Eng. Data 58(10):2828–2834 (2013).

- Motkuri RK, Annapureddy, HVR, Vijaykumar M, Schaef HT, Martin PF, McGrail BP, Dang LX, Krishna R, Thallapally PK, Fluorocarbon Adsorption in Hierarchical Porous Frameworks. Nat. Commun. 5(4368):1–6 (2014).

- Wanigarathna DKJA, Gao J, Takanami T, Zhang Q, Liu B, Adsorption Separation of R-22, R-32 and R-125 Fluorocarbons Using 4A Molecular Sieve Zeolite. Chemistry Select 1(13):3718-3722 (2016).

- Savitz S, Tieri SM, Gorte RJ, Grey CP, Huber R, Myers AL, Corbin DR, Siperstein FR, Adsorption of Hydrofluorocarbons HFC-134 and HFC-134A on X and Y Zeolites: Effect of Ion-Exchange on Selectivity and Heat of Adsorption. J. Phys. Chem. B 103(39):8283–8289 (1999).

- Akkimaradi BS, Prasad M, Dutta P, Srinivasan K, Adsorption of 1,1,1,2-Tetrafluoroethane on Activated Charcoal. J. Chem. Eng. Data 46(2):417–422 (2001).

- Saha BB, Habib K, El-Sharkawy II, Koyama S, Adsorption Characteristics and Heat of Adsorption Measurements of R-134a on Activated Carbon. Int. J. Refrig. 32(7):1563-1569 (2009).

- Loh WS, Kumja M, Rahman KA, Ng KC, Saha BB, Koyama S, El-Sharkawy II, Adsorption Parameter and Heat of Adsorption of Activated Carbon/HFC-134a Pair. Heat Transf. Eng. 31(11):910–916 (2010).

- Askalany AA, Salem M, Ismail IM, Ali AHH, Morsy MG. Experimental Study on Adsorption-Desorption Characteristics of Granular Activated Carbon/R134a Pair. Int. J. Refrig. 35(3):494-498 (2012).

- Loh WS, Ismail, AB, Xi B, Ng KC, Chun WG. Adsorption Isotherms and Isosteric Enthalpy of Adsorption for Assorted Refrigerants on Activated Carbons. J. Chem. Eng. Data 57(10):2766–2773 (2012).

- Saha BB, El-Sharkawy II, Thorpe R, Critoph RE, Accurate Adsorption Isotherms of R134a onto Activated Carbons for Cooling and Freezing Applications. Int. J. Refrig. 35(3):499–505 (2012).

- Attalla M, Sadek S, Experimental Investigation of Granular Activated Carbon/R-134a Pair for Adsorption Cooling System Applications. J. Power Energy Eng. 02(02):11–20 (2014).

- Zheng J, Vemuri RS, Estevez L, Koech PK, Varga T, Camaioni DM, Blake TA, McGrail BP, Motkuri RK, Pore-Engineered Metal-Organic Frameworks with Excellent Adsorption of Water and Fluorocarbon Refrigerant for Cooling Applications. J. Am. Chem. Soc. 139(31):10601–10604 (2017).

- Wanigarathna DKJA, Liu B, Gao J, Adsorption Separation of R134a, R125, and R143a Fluorocarbon Mixtures Using 13X and Surface Modified 5A Zeolites. AIChE J. 64(2):640-648 (2018).

- Zheng J, Barpaga D, Gutiérrez OY, Browning ND, Mehdi BL, Farha OK, Lercher JA, McGrail BP, Motkuri RK, Exceptional Fluorocarbon Uptake with Mesoporous Metal–Organic Frameworks for Adsorption-Based Cooling Systems. ACS Appl. Energy Mater. 1(11):5853–5858 (2018).

- Moon DJ, Chung MJ, Cho SY, Ahn BS, Park KY, Hong SI, Adsorption Equilibria of Chloropentafluoroethane and Pentafluoroethane on Activated Carbon Pellet. J. Chem. Eng. Data 43(5):861–864 (1998).

- Peng Y, Xu C, Xiao Q, Zhu W, Zheng X, Wang H, Zhong Y, Zhang F, Comparison Study on the Adsorption of CFC-115 and HFC-125 on Activated Carbon and Silicalite-1. Ind. Eng. Chem. Res. 49(20):10009–10015 (2010).

- Askalany AA, Saha BB. Experimental and theoretical study of adsorption kinetics of Difluoromethane onto activated carbons. Int. J. Refrig. 4 9:160-168 (2015).

- Lin SH, Lin RC, Adsorption of 1,1,1,2-tetrafluoroethane by various adsorbents. J. Environ. Eng. 125:1048-1053 (1999).

- Banker ND, Prasad M, Dutta P, Srinivasan K, Development and transient performance results of a single stage activated carbon – HFC 134a closed cycle adsorption cooling system. Appl. Therm. Eng. 30: 1126–1132 (2010).

- Lin SH, Lin RC, Prediction and experimental verification of HFC‐134a adsorption by activated carbons. J. Environ. Sci. Health 34(1):183-200 (1999).

- Askalany AA, Saha BB, Highly porous activated carbon based adsorption cooling system employing difluoromethane and a mixture of pentafluoroethane and difluoromethane. Heat Mass Transfer 53:107–114 (2017).

- El-sharkawy MM, Askalany AA, Harby K, Ahmed MS, Adsorption isotherms and kinetics of a mixture of Pentafluoroethane, 1,1,1,2-Tetrafluoroethane and Difluoromethane (HFC-407C) onto granular activated carbon. Appl. Therm. Eng. 93: 988–994 (2016).

- Esteves IAAC, Lopes MSS, Nunes PMC, Mota JPB, Adsorption of natural gas and biogas components on activated carbon. Sep. Purif. Technol. 62(2):281-296 (2008).

- Ribeiro RPPL, Esteves IAAC, Mota JPB, Two-column relay simulated moving-bed process for gas-phase separations. Sep. Purif. Technol. 182:19-28 (2017).

- Esteves IAAC, Gas separation processes by integrated adsorption and permeation technologies, Ph.D. Thesis, Universidade Nova de Lisboa (FCT/UNL), Lisbon, 2005

- Ravikovitch CPI, Neimark AV, Characterization of micro- and mesoporosity in SBA-15 materials from adsorption data by the NLDFT method, J. Phys. Chem. B 105: 6817–6823 (2001).

- Ribeiro RPPL, Antunes CL, Garate AU, Portela AF, Plaza MG, Mota JPB, Esteves IAAC. Binderless shaped metal-organic framework particles: Impact on carbon dioxide adsorption. Microporous Mesoporous Mater. 275:111-121 (2019)

- Camacho BCR, Ribeiro RPPL, Esteves IAAC, Mota JPB, Adsorption equilibrium of carbon dioxide and nitrogen on the MIL-53(Al) metal organic framework. Sep. Purif. Technol. 141(12): 150–159 (2015).

- Coupan R, Plantier F, Torré JP, Dicharry C, Sénéchal P, Guerton F, Moonena P, Khoukh A, Kessase SA, Hematie M, Creating innovative composite materials to enhance the kinetics of CO2 capture by hydroquinone clathrates, Chem. Eng. J. 325:35-481 (2017).

- Khaddour F, Knorst-Fouran A, Plantier F, Piñeiro MM, Mendiboure B, Miqueu CA, Fully Consistent Experimental and Molecular Simulation Study of Methane Adsorption on Activated Carbon. Adsorption 20(4):649–656 (2014).

- Coupan R, Plantier F, Torré JP, Dicharry C, Sénéchal P, Guerton F, Moonen P, Khoukh A, Kessas SA, Hemati M, Creating Innovative Composite Materials to Enhance the Kinetics of CO2 Capture by Hydroquinone Clathrates. Chem. Eng. J. 325(1):35–48 (2017).

- Do DD, Adsorption Analysis: Equilibria and Kinetics, in Chemical Engineer Series, Volume 2. Imperial College Press, London (1998).

- Wallace WE, NIST Chemistry WebBook, NIST Standard Reference Database Number 69. http://webbook.nist.gov/chemistry [accessed 12 September 2019].

- Mouahid A, Bessieres D, Plantier F, Pijaudier-Cabot G, A Thermostated Coupled Apparatus for the Simultaneous Determination of Adsorption Isotherms and Differential Enthalpies of Adsorption at High Pressure and High Temperature. J. Therm. Anal. Calorim. 109 (2):1077–1087 (2011).

- Dubinin MM, The potential theory of adsorption of gases and vapors for adsorbents with energetically nonuniform surfaces. Chem. Rev. 60(2):235-241 (1960)

- Dubinin MM, Adsorption in micropores. J. Colloids Interface Sci. 23(4):487-499 (1967).

- Dubinin MM, Physical Adsorption of Gases and Vapors in Micropores, in Progress in Surface and Membrane Science, ed by Cadenhead DA, Danielli JF. Academic Press, New York, pp 1-316 (1975).

- Ruthven DM, Principles of Adsorption and Adsorption Processes, John Wiley & Sons Inc, New York, (1984).

- Toth J, A Uniform Interpretation of Gas/Solid Adsorption. Adv. Colloid Interface Sci. 55:1-239 (1995).

- Ozawa S, Kusumi S, Ogino Y, Physical adsorption of gases at high pressure. IV. An improvement of the D–A adsorption equation, J. Colloids Interface Sci. 56(1):83-91 (1976).

- Dubinin MM, Astakhov VA, Description of Adsorption Equilibria of Vapors on Zeolites over Wide Ranges of Temperature and Pressure. Adv. Chem. Ser. 102:69-85 (1971).

- Thommes M, Kaneko K, Alexander VN, James PO, Rodriguez-Reinoso F, Rouquerol J, Kenneth SWS, Physisorption of gases, with special reference to the evaluation of surface area and pore size distribution (IUPAC Technical Report), Pure Appl. Chem. 87(9-10):1051-1069 (2015).

- Nabais AR, Ribeiro RPPL, Mota JPB, Alves VD, Esteves IAAC, Neves LA, CO2/N2 gas separation using Fe(BTC)-based mixed matrix membranes: A view on the adsorptive and filler properties of metal-organic frameworks, Sep. Purif. Technol. 202:174-184 (2018).

- Woog GO, Wood, Affinity coefficients of the Polanyi/Dubinin adsorption isotherm equations. A review with compilations and correlations, Carbon 39(3):343-356 (2001).

- Wood GO, Activated carbon adsorption capacities for vapors, Carbon 30(4): 593-599 (1992).

- Dubinin MM, Timofeev DP, Adsorption of vapors on active charcoals in relation to the properties of the adsorbate, Compt. Rend. Acad. Sci. URSS 54: 701-704 (1946).

- Myers AL, Prausnitz JM, Thermodynamics of Mixed-Gas Adsorption. AIChE J. 11(1):121–127 (1965).

- Myers AL, Adsorption of Gas Mixtures - a Thermodynamic Approach. Ind. Eng. Chem. 60(5):45-49 (1968).

| Table 1. Chemical structures and properties of the fluorinated gases studied in this work. The vapor pressure, Ps, at 303.15 K is reported in MPa, the critical volume, Vc, in cm3/mol, and the critical temperature, Tc, in K. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Gas | Chemical structure | Ps | Vc | Tc |
| R-32 (Difluoromethane) |  | 1.93 | 120.8 | 351.26 |
| R-125 (Pentafluoroethane) |  | 1.57 | 211.3 | 339.17 |
| R-134a (1,1,1,2-Tetrafluoroethane) |  | 0.77 | 198.8 | 374.21 |

| Table 2. BET surface area, SBET (m2/g), and specific pore volume, vp (cm3/g), of the ACs. |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | EcoSorb | BAC | AC1 | AC2 |
| SBET | 1100 | 1250 | 1695 | 1280 |
| vp | 0.52 | 0.49 | 0.76 | 0.68 |

Figure 1. Pore size distribution of AC1 (green triangles), AC2 (pink diamonds), BAC (blue circles), and Ecosorb (red squares), determined by deconvolution of the N2 adsorption isotherm at 77 K using standard methods based on the Non-Localized Density Functional theory (NLDFT).

Figure 2. Adsorption equilibrium isotherms of R-32 on AC1 (green triangles), AC2 (pink diamonds), BAC (blue circles), and Ecosorb (red squares), at 283.15 K (A, B), 303.15 K (C, D), and 323.15 K (E, F). The dashed lines represent the data fittings with the dimensionless form of Tóth’s model (eqn. 17). The right-hand-side plots use a logarithmic pressure scale.

Figure 3. Adsorption equilibrium isotherms of R-125 on AC1 (green triangles), AC2 (pink diamonds), BAC (blue circles), and Ecosorb (red squares), at 283.15 K (A, B), 303.15 K (C, D), and 323.15 K (E, F). The dashed lines represent the fittings with the dimensionless form of Tóth’s model (eqn. 17). The right-hand-side plots use a logarithmic pressure scale.

Figure 4. Adsorption equilibrium isotherms of R-134a on AC1 (green triangles), AC2 (pink diamonds), BAC (blue circles), and Ecosorb (red squares), at 283.15 K (A, B), 303.15 K (C, D), and 323.15 K (E, F). The dashed lines represent the fittings with the dimensionless form of Tóth’s model (eqn. 17). The right-hand-side plots use a logarithmic pressure scale.

Figure 5. Isosteric heats of adsorption of R-32 (A), R-125 (B), and R-134a (C) at 323.15 K on AC1 (green triangles), AC2 (pink diamonds), BAC (blue circles), and Ecosorb (red squares).

Figure 6. Determination of αT for R-32 adsorption on AC2. The molar volume of the adsorbed phase, va(T), is such that a plot of W≡vaq as a function of ϕ≡RT ln(fs/f) produces a single characteristic curve with minimum data scatter that satisfies the condition limϕ→0 θ=1 when Ws is equal to the specific pore volume, vp. Data are represented for 283.15 K (red circles), 303.15 K (blue triangles), and 323.15 K (green squares). Data obtained with α=1 are shown as empty symbols on the right-hand-side vertical axis, which is shifted upwards by 0.4 units for better visualization. Data obtained with a corrected value of α are shown as full symbols.

Figure 7.  Fractional loading or pore volume filling, θ=W/Ws ≡qva/vp, as a function of reduced pressure, x=P/Ps, for R-32 adsorption on AC1 at 283.15 K (red circles), 303.15 K (blue triangles), and 323.15 K (green squares).

Figure 8. Characteristic curves obtained by superimposing the experimental adsorption data of R-32, R-125, and R-134a at 283.15 K, 303.15 K and 323.15 K on AC1 (A, B), AC2 (C, D), BAC (E, F), and Ecosorb (G, H) into a single temperature-independent curve. The characteristic curves were fitted to eqn. 23 (represented as dashed lines). The right-hand-side plots use a logarithmic scale of fractional volume filling.

Figure 9. Selectivity of AC1, AC2, BAC, and Ecosorb to R-125 over R-32 as function of pressure at 303.15 K, for the equilibrium gas phase composition of bulk the R-410A mixture (yR-32=0.7 and yR-32=0.3).

Figure 10. Selectivities of AC1, AC2, BAC, and Ecosorb activated carbons to: R-125 over R-32 (A); R-134a over R-32 (B); and R-134a over R-125 (C), for the commercial R-407F gas mixture (yR-32=0.47, yR-125=0.21, and yR-134a=0.32), as a function of pressure at 303.15 K. For a better visualization, the inset on each graph shows a zoomed-in view of the curves for the lowest values of the selectivity.